- Research activity

The aim of my project is to investigate the procedure used in the preparation, firing and decoration of Red Slip Ware, a typical Phoenician ceramic production.

During the three years of my PhD, I carried out the following research activities:

- Bibliographic research;

- Petrographic analyses of the Phoenician ceramics in thin sections;

- XRPD, SEM-EDS and EMPA analyses on the ceramic samples from seven archaeological sites;

- LIBS (laser induced breakdown spectroscopy) analyses on the superficial decoration of the artefacts;

- Electrochemical analyses by VIMP (Voltammetry of Immobilized Microparticles), performed during a research period of 3 months at Facultat de Química of the Universitat de València (València - Spain);

89 Phoenician Red Slip Ware samples, collected from seven archaeological sites of the Mediterranean area, have been analysed to achieve the aim of the project.

Moreover, I participated to the excavation during the archaeological mission of Sapienza- Università di Roma to Motya (Sicily- Italy), in September 2017 and I spent a research period at Museum of Cadiz (Cadiz - Spain), in May 2018.

I have joined, as a participant, the project “Grandi Scavi” of Sapienza- Università di Roma entitled “Motya: investigating ancient Mediterranean cultures. Excavation, interdisciplinary study and analyses, interpretation and outreach”.

Finally, I have won a grant for international mobility of PhD students with the project “GEARCH - Studio multianalitico per la provenienza di materiali antichi e moderni negli ambiti della geologia e dell'archeometria”.