- Research activity

My research activity aims at the implementation and validation of new non-destructive Nuclear Magnetic Resonance (NMR) protocols for investigating archaeological and historical remains and their consolidating, protecting and cleaning materials. The main material investigated in my research is modern and ancient wood.

For this purpose, I’m using both high-field NMR and low-field portable NMR spectrometers. Specifically, I’m working with high-field spectrometers in order to carry on two main research lines:

- The first is based on the improvement of the in plane resolution of Magnetic Resonance Imaging (MRI) to obtain a complete virtual histology of wood in a non-destructive modality. MR-images can reveal diagnostic characters of wood for the species identification as showed in Capuani et al. 2020 [1] where images of modern and archaeological woods were obtained with a minimum resolution of 20x20 µm2. This allowed to observe many anatomical elements and degradation effects with the great advantage of not mechanically cutting the sample.

- The second research line exploits diffusion-NMR principles to extract morphological and topological information from wood microstructure, such as pores diameter, cell wall permeability, pores interconnection, tortuosity [2]. In this sense, I’m studying modern and archaeological (Roman age) wood small samples with non-destructive high-field techniques in order to characterize their morphology and study their degradation. As presented in my work Stagno et al. 2020 [3], the combined use of diffusion-NMR and micro-MRI is a useful tool to reveal decay processes and diagnostic features of wood, suggesting that parameters as tortuosity and water diffusion coefficient are widely affected by morphological variations of the sample.

However, to overcome sample size limitations imposed by the use of non-portable high-field instruments, the same protocol is going to be translated on portable low-field spectrometer in order to obtain, in a completely non-invasive way from any size samples, the same information together with the characterization of the water compartmentalization by the measurement of relaxation parameters (such as the longitudinal relaxation time T1 and the transversal relaxation time T2). Moreover, for exploiting the great potential of portable NMR for Cultural Heritage artworks, new approaches will be also tested. Particularly, portable NMR is being used for monitoring the effect of relative humidity (RH) variations on the water clusters of different wood species. The measurement of T1 and T2 at different RH values and the correlation of T1 vs. T2 is utilized for discriminating softwoods and hardwoods. Two-dimensional correlation T1-T2 and D-T2 experiments are tested on the portable NMR to increase the resolution of the relaxation components in respect to the 1D experiments [4]. Furthermore, I’m expanding the application of portable NMR to other porous system, such as stones, for their characterization and to assess the cleaning efficacy of PVA-borax hydrogel in removing stains and dust from stone surfaces [5, 6].

In 2021, I obtained funding for a research project concerning the synthesis, NMR characterization and application of lignin nanoparticles as a potential consolidating material for wood.

- Research products

- Capuani S, Stagno V, Missori M, Sadori L, Longo S. High‐resolution multiparametric MRI of contemporary and waterlogged archaeological wood. Magnetic Resonance in Chemistry 2020; 58 (9): 860-869.

- Stagno V, Egizi F, Corticelli F, Morandi V, Valle F, Costantini G, Longo S, Capuani S. Microstructural features assessment of different waterlogged wood species by NMR diffusion validated with complementary techniques. Magn Reson Imaging. 2021 Nov;83:139-151. doi: 10.1016/j.mri.2021.08.010.

- Stagno V, Longo S, Capuani S. Effect of age on Pine wood microstructure studied by micro-MRI and diffusion-NMR. IMEKO TC-4 2020 International Conference on Metrology for Archaeology and Cultural Heritage Proceedings 2020; pp. 570-574, ISBN: 978-92-990084-9-2.

- Stagno V, Mailhiot S, Capuani S, Galotta G, Telkki V-V. Testing 1D and 2D single-sided NMR on Roman Age waterlogged woods. Submitted to Journal of Cultural Heritage.

- Stagno V, Genova C, Zoratto N, Favero G, Capuani S. Single-Sided Portable NMR Investigation to Assess and Monitor Cleaning Action of PVA-Borax Hydrogel in Travertine and Lecce Stone. Molecules. 2021; 26(12):3697. https://doi.org/10.3390/molecules26123697

- Stagno V, Ciccola A, Curini R, Postorino P, Favero G, Capuani S. Non-Invasive Assessment of PVA-Borax Hydrogel Effectiveness in Removing Metal Corrosion Products on Stones by Portable NMR. Gels. 2021; 7(4):265. https://doi.org/10.3390/gels7040265